	Test Result Summary

	 
	 
	 
	 
	 

	 
	Test Type
	S-Fill
	Sand
	Rubber

	1
	Microbiological Analysis
	.007% or
	68.18%
	81.82%

	 
	using ATCC164404AN
	negligible
	 
	 

	 
	spore growth after contamination
	 
	 
	 

	 
	 
	 
	 
	 

	2
	Abrasiveness 
	17±
	N/A
	31.9±

	 
	ASTMF1015
	 
	 
	 

	 
	 
	 
	 
	 

	3
	Radiant Panel Flammability Test
	Best Possible
	N/A
	will not pass

	 
	ASTME-648, NFPA253 & FTM372
	1.02
	 
	<.22

	 
	 
	 
	 
	 

	4
	G-Max ASTMF355
	 
	 
	 

	 
	Turf/Sport Drain Pad over concrete
	100
	N/A
	N/A

	 
	Turf/Sport Drain Pad over soil 95%C
	98
	N/A
	N/A

	 
	 
	 
	 
	 

	5
	Shoe Traction ASTM F1551
	 
	 
	 

	 
	Dynamic Coefficient Friction
	 
	 
	 

	 
	Dry Football
	0.86
	N/A
	0.81

	 
	Wet Football
	0.80
	N/A
	N/A

	 
	Dry Soccer
	0.82
	N/A
	N/A

	 
	Wet Soccer
	0.77
	N/A
	N/A

	 
	 
	 
	 
	 

	6
	Sports Surface Simulated Sunlight Test
	93.62˚F
	N/A
	141.88˚F

	 
	Temperature after 30 minutes absorption
	 
	 
	 

	 
	of 250W heat lamp
	 
	 
	 

	 
	 
	 
	 
	 

	7
	Heavy Metal Test
	None
	N/A
	Zinc

	 
	Method 6010 & 7470
	 
	 
	 

	 
	 
	 
	 
	 

	8
	Water Flow BS7044
	42 in/hr
	N/A
	N/A

	 
	 
	 
	 
	 

	9
	API Turbidity Test for Dust
	23.5
	250
	335

	 
	 
	 
	 
	 

	
	 
	 
	 
	 

	Test results provided by Testing Services, Inc., NAMSA and Analytical Industrial Research Laboratories, Inc.


